# Materials Testing Report

Report Number: MTR-2026-0091

Client: Falcon Aerospace Components Ltd.

Test Standard: ASTM E8 / ASTM E18

Sample Batch: FA-TI6AL4V-0326

## Tensile Test Results

| Specimen ID | Yield Strength (MPa) | Tensile Strength (MPa) | Elongation (%) |
| --- | --- | --- | --- |
| TI-001 | 880 | 950 | 14.2 |
| TI-002 | 875 | 945 | 13.8 |
| TI-003 | 890 | 960 | 14.5 |

## Hardness Test Results

| Specimen ID | Rockwell C (HRC) | Result |
| --- | --- | --- |
| TI-001 | 36 | Pass |
| TI-002 | 35 | Pass |
| TI-003 | 37 | Pass |

## Conclusion

All three specimens from batch FA-TI6AL4V-0326 meet the minimum yield strength requirement of 830 MPa specified in the client's engineering drawing.

Tested by: Priya Nair, Senior Materials Engineer

Reviewed by: Tom Hendricks, Lab Quality Manager